We proposed to study a recently discovered phenomenon called ‘flash’ whereby a crystal is placed under a moderate electric field at high temperature. At fixed temperature, increasing the E-field over a critical value results in a sudden drop in the resistivity of the crystal and a metallic current begins to flow. Alternatively, we can hold the E-field fixed and raise the temperature over a critical value. Once the resistivity drops, a metallic current begins to flow and the material emits light (“flashes”) in a electroluminescence-like phenomenon. Flash occurs in many materials under a wide range of conditions. To date, flash is more-or-less completely enigmatic.
We planned diffuse neutron scattering experiments to the examine the structure of a crystal during flash. Our primary goals were (i) to extend what is known about flash to a technologically relevant material, relaxor PMNPT, (ii) to study the effect of simultaneous E-field and B-field, and (iii) to develop non-equilibrium models for the physics of flash based on what is learned in steps (i) and (ii). To some extent, we have addressed or begun addressing each of these goals. For all of them, we have actionable plans for how to continue to study these problems in the future.
In the case of (i), we performed in-situ neutron diffuse scattering measurements for PMNPT and several other samples: SrTiO3, TiO2 with different flash conditions, and La2CuO4 (which broke during the experiment). These results were discussed extensively in the mid-progress report, so I will only briefly summarize them here. These experiments were more-or-less null (as discussed in the mid-project report). In short, for PMNPT and SrTiO3 there was no visible diffuse scattering suggesting either the absence of defects (unlikely), uncorrelated defects (possible), or that defects formed only near the surface of samples these samples (likely). In TiO2, diffuse scattering suggested the formation of bulk Wadsley defects (these data support earlier results that we are publishing). A reasonable course of action to identify defects near the surface would be X-ray diffuse scattering, though this will be complicated by the low sensitivity of X-rays to oxygen. I may attempt this in the future.
Our diffuse scattering results on TiO2 are consistent with our hypothesis (that is shared by others in the field) that the formation of oxygen defects is relevant for flash. On the other hand, the absence of diffuse scattering in the other samples we measured doesn’t support this. However, these null-results don’t necessarily contradict this hypothesis either. As mentioned above, it may be possible that oxygen defects exist, but are randomly distributed or only present near the surface (in either case, we wouldn’t see this with neutron scattering).
An interesting result (from data on TiO2) is that, while the shape of diffuse scattering isn’t affected by the in-situ current, the magnitude of diffuse scattering is (see additional material). Moreover, Bragg peaks are correlated with current density. We were able to use the integrated Bragg peaks vs. current to estimate the temperature of in-situ flashing samples (see additional material and see below). This latter result serves a good proof of concept for follow up inelastic scattering experiments that we have planned later this year to more precisely measure the temperature. Moreover, it shows that we can use these in-situ measurements to understand the non-equilibrium physics of flash.
A side-effect of the experiments at ORNL is that we noticed a non-trivial change in the flash conditions when the sample is flashed in vacuum (the in-situ furnaces at ORNL at high vacuum). Inspired by this, I oversaw the procurement of a vacuum tube furnace by our lab at the University of Colorado Boulder (CU). I designed modifications to the furnace that enabled using a custom (also designed by me!) flash stick at CU. My lab mates are currently making heavy use of this to explore the role of sample environment on the physics of flash. Moreover, I have plans to measure the light emission spectrum vs. sample environment and to do in-situ Raman measurements in the vacuum furnace at CU, among other things. I will graduate this Fall (2024) and will re-join my group as post-doc to continue this work.
Regarding the simultaneous E- and B-field: my lab mates at the University of Colorado (CU) did preliminary testing on the affect of B-field during flash. The originally published experiment used an EM-coil; we attempted to replicate the experiment with a permanent magnet. We found no affect due to magnetic field. We supposed that the coil simply acts as a heating element rather than the B-field being significant. Currently, my lab mates are trying to replicate the experiment using a coil and I will participate in this work in the future. So far, the reported experimental set up doesn’t agree with the claimed physics and we are skeptical of this effect. Based on our own inconclusive results with B-field, and considering the technical complexity of a simultaneous E- and B-field apparatus, we decided not to pursue such a device at this time. Rather, we used our funds to invest in a new in-situ E-field apparatus to use at the HFIR source at ORNL for triple-axis neutron scattering experiments. We commissioned the ORNL sample-environment team to designed the new sample stick and we paid to have it manufactured (completed in March 2024). The goal of this new sample stick is to study the non-equilibrium dynamics during flash. In the future, if we can independently prove that the B-field is significant (which my group is trying to do with our in-house vacuum furnace at CU), we will commission a new stick and will apply for beam time through the usual channels.
To some extent, we were able to make claims about non-equilibrium physics during flash. Specifically, we are able to estimate to the temperature of the in-situ flashing sample based on our neutron scattering measurements. See the additional material for details. Currently, the temperature of an in-situ sample is completely unknown and attempts to measure it are dubious: some groups have measured the light spectrum and fit it as a black body. This is a poor approximation (the crystals are not close to perfect black bodies and also exhibit absorption/emission lines). Due to data quality limitations, our estimate is not better, but does serve as a good proof of concept for follow up experiments.
To that end, we have submitted (accepted) proposals to ARCS at the SNS and TAX at HFIR to do inelastic scattering measurements using the in-situ apparatuses we commissioned. Being able to accurately measure the temperature and, more importantly, correlate it with the current density will provide valuable insight on flash. The specific goals are (a) to look for significant changes in the phonon spectra during flash and (b) to measure the temperature via the phonon populations. For (a) we are interested in either changes in phonon energies or phonon line-shapes as well the appearance of new peaks. Changes in phonon energies and widths are directly related to interactions between electrons and phonons, or electrons and photons (the E-field), enabling us to directly relate the experiment to non-equilibrium models for the physics. Most likely, the former is the most important effect since there is a large current flowing during flash. On the other hand, if new peaks show up in the spectrum, this implies a change in the structure (i.e. a change in the atomic displacement pattern). While not a direct probe of the non-equilibrium dynamics, this is an interesting result if observed.
For (b), we want a way to precisely measure the temperature. Phonons are Bosons, so follow the Bose-Einstein distribution. i.e., the intensity of peaks in the neutron spectrum is related to the temperature of the sample. While flashing, the temperature of the sample increases (Joule heating). We have (successfully) proposed to very carefully measure the peak heights on both ARCS and TAX at ORNL. These experiments will be completed this year. We mention that we attempted a related experiment on ARCS in June 2024 that was unsuccessful due to equipment failure (part of the spectrometer wouldn’t move into place). This was discussed in detail in the mid-project report, so I won’t belabor it here.
We have also attempted to use our diffuse scattering data to refine the structure of TiO2 during flash and correlate any in-situ structural changes with flash. i.e. we want to ‘fit’ the real Bragg scattering intensities by letting atomic displacements in the unitcell be free parameters. Note, we haven’t attempted this for PMNPT or SrTiO3 yet since TiO2 is proving more fruitful overall. I will look into the other datasets when we have finished with TiO2. Refining the structure involves integrating Bragg peaks from the diffuse scattering data. Unfortunately, the Bragg peak intensities are too noisy to make any significant progress. The poor data quality is due to ‘wobble’; it is very difficult to center a sample in the in-situ apparatus and, while rotating the sample during scattering measurements, the sample ‘wobbles’ around the axis of rotation. The resulting displacement in the sample position apparently has a significant effect on the Bragg peak intensities. Still, we are able to use the trend in peak intensities with current to estimate the temperature (see additional materials).